Sapphire Optical Lens Spectral Transmittance Test Report
Report No.: SAPP-LENS-2026-TEST-XXXX Manufacturer: Felix Glass Co., Limited Test Equipment: UV-IR spectrophotometer, laser interferometer
1 Test Sample Info
Product: Sapphire half ball lens, D=8mm, double-side IR AR coating Substrate: C-plane single crystal sapphire
2 Test Result Data
	Waveband
	Average Single-Surface Transmittance
	Requirement Standard
	Result

	1.0μm–2.0μm
	93.1%
	≥92%
	Pass

	2.0μm–3.5μm
	92.8%
	≥92%
	Pass

	3.5μm–5.0μm
	92.2%
	≥90%
	Pass


3 Surface Flatness Inspection
Test Wavelength: 632.8nm He-Ne laser Measured flatness: λ/4.2, meet customer λ/4 tolerance demand.
4 Coating Adhesion Test
3M tape scratch test, no coating peeling or falling off.
5 Test Conclusion
This batch of sapphire optical lenses meets industrial precision fiber coupling equipment optical index standards, can be delivered for OEM assembly. Inspector: Optical QC Engineer Date: YYYY-MM-DD
